松辽盆地嫩江组油页岩有机质热解动力学模型

摘要：原位转化技术是松辽盆地嫩江组中低熟页岩油藏最具前景的开采技术，转化过程涉及油页岩中有机质多步热解反应的耦合，建立可靠的有机质热解动力学模型需对该过程进行解耦。首先对0.5、1、2、4℃/min升温速率下嫩江组油页岩热解的热重曲线开展了反卷积分峰，基于分峰精度以及活化能均一性判据，将有机质热解过程解耦为三步反应并获得了各步反应的热解特性。随后对三步反应分别开展了动力学分析，获得的动力学方程对三步反应过程的预测精度均高于0.96。结合各反应对应的产物分布及在有机质热解过程中的权重，建立了嫩江组油页岩多反应耦合有机质热解动力学模型。该模型对于0.2-4℃/min范围内有机质热解过程的预测精度高于0.994，远超有机质热解总包反应动力学模型（预测精度0.932）。采用该模型可较好地预测不同加热历程下油页岩有机质热解过程及产物组成，对于该油藏原位转化技术的开发有重要的指导作用。

关键词：中低熟页岩油；原位转化；热解；解耦；动力学模型；化学反应

中图分类号：TE 662         文献标志码：A

随着美国页岩油气革命的成功实现[1]，世界各国开始将目光转移至页岩油等非常规油气资源的勘探开发[2-5]。松辽盆地嫩江组页岩油是中国中低熟页岩油藏的重要组成部分[6]，可采资源量在100－150亿吨，若能实现开采，将大幅提升中国的能源安全保障能力。中低熟页岩油由油页岩中的重质沥青与未转化的固体有机质构成，埋深大于1000m，开采难度较大。因此，中国石油勘探开发研究院提出采用原位转化技术开发该类油藏[6-8]，即通过对油页岩进行地下原位加热，使重质油与固体有机质转化为轻质油气继而开采。油页岩有机质热解是该技术实现产油产气的核心化学过程。因此，建立能够描述松辽盆地嫩江组油页岩原位转化过程并预测产物分布的有机质热解动力学模型，对原位转化技术的开发具有重要的指导意义。

通常采用热重分析方法研究油页岩热解特性并建立动力学模型。从油页岩热解的热重曲线看，页岩热解可分为三个阶段[9-11]，按照温度由低到高，分别为水分蒸发阶段、有机质热解阶段和矿物热解阶段。而不同油页岩由于组分的差异，各阶段的热解失重行为具有显著区别[12-21]。例如，吉木萨尔油页岩、共榔头油页岩、欧瑞美油页岩在水分蒸发阶段的失重率分别为3，6.07，1.4%，在有机质热解阶段分别为12，24.5，14%，在矿物热解阶段分别为4，5.5，33.4%[16-18]。这三种油页岩在各个失重阶段的温度范围也并不一致。因此，对于不同油页岩，需要针对性地建立对应有机质热解动力学模型。

建立油页岩有机质热解动力学模型通常采用常压多升温速率下油页岩热解的热重实验数据。与实验室开展的热重实验条件相比，地下原位转化在高压和缓慢升温速率下进行[19,22 31]。对于油页岩有机质的热分解过程，压力主要影响产物的传质。由于热重实验中采用的样品量很少，传质对反应影响可忽略，因而采用常压下热重实验数据获得的反应动力学模型可用于高压环境。但地下原位转化的慢升温速率（0.000 35-0.7℃/min）[31]对多反应耦合过程的分析方法提出了挑战。目前大部分油页岩的热重分析采用10℃/min以上的升温速率[12-14]。油页岩有机质热解过程涉及多步反应[23-29]，在快速升温过程中，各步反应耦合在一起，容易形成在有机质热解阶段单失重峰的特征，因此学者们常采用单步总包反应模型来描述油页岩的有机质热解动力学过程[10,14,18,30,31]。然而，松辽盆地嫩江组油页岩在有机质热解阶段呈现重叠失重峰的特征[35]，表明该油页岩在有机质裂解过程存在多个主要反应，在地下原位转化的缓慢升温过程中，多步反应势必被进一步拉开，其差异性将进一步显现，使得单步总包反应的假设不再适用。因此，为了构建适用于地下原位转化缓慢升温过程的有机质热解动力学模型，需要对多步反应耦合的热解过程进行解耦，并分别建立各步反应的动力学方程。

在基于热重曲线对多步反应进行解耦时常采用反卷积分峰方法，即将重叠峰通过多个峰形函数分解成多个单失重峰，并将每个失重峰视作一个单步独立反应。一般基于拟合精度确定分峰结果[25,32-34]。但从Bai和Alves等学者的研究[32,34]中发现，基于分峰结果采用等转化率法计算得到的活化能随转化率变化波动幅度大，不符合单一独立反应的特征[32]，因此仅基于拟合精度并不一定能够准确解耦多步反应。而热解过程多步反应的有效解耦，是建立适用于宽升温速率下有机质热解动力学模型的重要基础。此外，需要指出的是，目前基于热重分析建立的油页岩热解动力学模型，由于未能与各步反应产物进行关联，缺乏预测热解产物分布的功能。而不同油页岩的热解产物组成存在较大差异，例如，大城子油页岩热解产物中油产物占比为59%，远高于共榔头油页岩的30%左右，两种油页岩油产物中的烷烃/芳香烃比值相差近一倍[24]。因此需将有机质热解动力学模型与对应的油页岩热解产物结合从而实现对产物分布的准确预测。

采用原位转化技术开采特定中低熟页岩油藏时，针对性地建立能够准确描述油页岩热解过程的动力学模型对于技术开发至关重要。针对有机质热解过程存在多步反应耦合的松辽盆地嫩江组油页岩，我们前期工作中提出将其有机质热解过程解耦为三个独立反应并探明了各步反应产物分布[35]。本文在此基础上，对松辽盆地嫩江组油页岩有机质热解阶段的热重曲线进行分峰，获得了不同升温速率下三步反应各自的失重曲线，并据此建立了各步反应的动力学方程；结合三步反应对应的产物分布及其在有机质热解过程中的权重，建立了嫩江组油页岩多反应耦合有机质热解动力学模型，并对该模型在预测不同升温速率下有机质热解过程的精度进行了分析。本文建立的嫩江组油页岩有机质热解动力学模型，既可高精度预测有机质转化程度，又可预测热解产物分布，对于采用原位转化技术开采松辽盆地嫩江组油页岩油藏具有重要指导意义。

- 研究方法

  - 样品与热重实验

研究所用油页岩样品取自松辽盆地嫩江组二段，深度1 880m左右，TOC含量介于8.79-9.23%之间，样品性质与制备方法的详细信息可参见[35]。采用热重分析仪在0.2-4℃/min的升温速率下对油页岩样品开展了热解实验，操作步骤如下：每次使用10 mg左右的油页岩粉体，采用热重分析仪(TGA，TGA/DSC3+，Mettler Toledo)开展从50-750℃的程序升温热解实验。300℃前主要为水分蒸发的物理过程，因此采用20℃/min的升温速率升至300℃，随后以0.2℃/min的升温速率从300℃加热至750℃。以上操作均在氮气氛围下进行，流速维持在50 ml/min。

  - 油页岩多步热解反应解耦方法

## 采用改进的反卷积分峰方法对不同升温速率下DTG曲线进行处理从而解耦多步耦合反应。首先基于调研结果确定油页岩的热解反应数量范围（对应拟合峰个数），对DTG曲线采用不同拟合峰数拟合。拟合峰的函数方程如式（1）所示，其中a0为振幅，a1为中心，a2为宽度，a3为形状参数，下标i代表第i个拟合峰。所有拟合峰叠加之后即可得到拟合曲线。选出拟合曲线与实验曲线相关系数最高的几种的分峰方案，随后采用等转化率法计算所有拟合峰在转化率在[ 0.1, 0.9 ]范围内变化时的活化能，选择不同转化率下各峰活化能波动范围小于10%的分峰方案作为最终结果。如不同分峰方案的结果均满足上述指标，则选择活化能平均波动最小的拟合峰数。

## .      (1)

## 由分峰结果获得各步反应的热解失重特性后，基于各反应峰值温度，采用固定床加热系统开展分阶段恒温热解实验并表征热解产物，从而获得各反应对应产物分布。具体解耦方法可参见[35]. 在前期工作中，我们将该油页岩有机质热解过程准确地解耦为了三步反应，分别为干酪根的转化，以及沥青质的一次、二次裂解并获得了各步反应的产物分布，以上结果将用于建立有机质热解动力学模型。

  - 动力学建模

基于采用反卷积分峰获得的0.5、1、2、4℃/min升温速率下三步反应的热重曲线，分别建立各步反应的动力学模型。动力学模型的三个主要参数分别为指前因子A、活化能E与机理函数f(α)。通过比对单步反应动力学模型计算结果与实验数据，对动力学参数进行迭代求解以减小偏差，从而获得拟合精度最优的动力学参数组合。由于直接拟合计算量大、耗时长，我们首先通过STK方法[36]、Coats-Redfern(CR)方法[37]以及动力学补偿关系[38-39]来确定各步反应动力学参数的分布范围与初值，随后再进一步优化，可以显著缩短计算耗时。结合最终各步反应的动力学方程与各步反应对应产物组成，便可建立油页岩有机质热解动力学模型。需要一提的是，0.2℃/min下的热重结果用于证明所建立动力学模型对更低升温速率下油页岩有机质热解过程的预测能力。具体方法见1.3.1-1.3.2节。

1.3.1 单步反应动力学参数的确定

建立有机质热解动力学模型的第一步需要计算各步反应的动力学参数。对于单步反应，动力学参数的计算流程如图1所示。

图1 单步反应动力学参数计算流程图

首先采用等转化率法确定反应活化能E的分布范围及初值。现有研究指出[34]，相比于其他的等转化率法[36,40-41]，STK方法具有更低的计算误差，因此采用STK方法对不同转化率下的活化能进行计算。计算反应活化能时，转化率范围取[0.1-0.9]，间隔为0.1，通过0.1-0.9转化率内活化能上下限便可确定活化能的分布范围。取9个转化率下活化能的平均值作为反应活化能初值—E。

其次确定指前因子A初值。由于动力学补偿效应的存在，指前因子的对数形式lnA与活化能E具有线性相关性[38-39]。因此指前因子可作为活化能的函数，其参数范围也可由活化能分布范围确定。动力学补偿效应方程可基于Coats-Redfern（CR）方法计算结果得到。将—El代入，便可获得指前因子初值。

最后是机理函数f(α)。由于油页岩反应过程复杂，本文根据国际热分析和量热联合会（ICTAC）的研究[42]选取式（2）作为反应机理函数的数学形式。式中的C、o、n、p为需要确定的参数。

.     (2)

各步反应的机理函数初值设定为一级反应模型，即f(α)=(1-α),因此C、o、n、p的初值分别为1、0、1、0。关于各参数的优化范围，通常认为反应级数不会超过5级反应[9,14 31,44]。结合该假设与现有机理函数数学形式，确定机理函数各参数的分布范围如表1所示。

表1 机理函数的参数优化范围

| 参数 | C | o | n | p |
| --- | --- | --- | --- | --- |
| 优化 范围 | [0, 5] | [-1, 1] | [-1, 5] | [-1, 1] |

采用上述方法确定了各反应动力学参数的分布范围与初值后，需进一步优化。C、o、n、p、E、A 是动力学模型中待优化的6个参数，考虑到指前因子基于动力学补偿效应可作为活化能的函数，因此不作为一个单独的优化参数。基于获得的6个参数初值，预测不同温度下的反应转化率，并与实验数据比对计算预测误差(即目标函数)。随后，根据贝叶斯优化算法在设置的参数范围内寻找能够最有效降低预测误差的参数迭代方向，逐步迭代参数并计算目标函数(每一步迭代后，指前因子会随活化能进行更新，用于计算目标函数)。最后在设定的迭代步数内预测误差最小的动力学参数Cf、nf、of、pf、Ef、Af将作为最终结果，下标f代表最终值。算法目标函数ε如式（3）所示，k代表第k个升温速率，上标Exp和Sim分别代表实验与模型预测值。

.        (3)

目标函数的计算过程如下：以0.01为步长，在转化率0.01到0.99的范围内分别确定99个转化率对应温度，采用动力学模型计算这些温度下对应转化率的预测值，将这些温度点下对应转化率实验值与模型计算值之差的绝对值之和作为该升温速率下动力学模型的预测误差。将4个升温速率下的动力学模型预测误差之和作为目标函数。

各步反应动力学方程的预测精度可通过对比转化率随温度变化的预测曲线与实验曲线的相关系数R2来评估，单步反应的实验曲线可根据油页岩热解DTG曲线分峰得到。

    - 油页岩多反应耦合有机质热解动力学模型的建立与评价

| (a) 有机质热解 | (b) 干酪根的转化 |
| --- | --- |
| (c) 沥青质的一次裂解 | (d)沥青质的二次裂解 |
| 图2 0.5-4℃/min升温速率下嫩江组油页岩有机质热解以及解耦三步反应的失重速率曲线 |  |

得到各步反应动力学参数后，需要将三步反应动力学方程按照一定权重进行叠加，从而建立油页岩有机质热解动力学模型，预测油页岩有机质转化率αO。αO定义为当下有机质失重量与有机质完全反应对应失重量的比值，α代表转化率，下标O代表油页岩有机质。本文采用式（4）计算不同时刻的油页岩有机质转化率，m代表油页岩当下质量，m0代表油页岩初始质量，Yl代表第l个反应对应的热解产物总产量（失重率）占初始油页岩质量的百分比，mDry代表已经经历水分蒸发阶段的油页岩质量，对应热重实验中300℃下油页岩的质量。由于嫩江组油页岩有机质热解阶段由三步反应组成，因此油页岩有机质转化率与三步反应对应转化率相关，具体可用式（5）表示。wl为各步反应所占权重。各反应的权重可根据该反应失重率Yl与油页岩有机质热解阶段总失重率的比值确定，具体计算方式可参照式（6）。将式（6）对时间微分，便可得到油页岩多反应耦合有机质热解动力学模型，如式（7）所示。动力学模型的预测精度可通过比较油页岩有机质热解阶段有机质转化率变化实验曲线与模型预测曲线的相关系数R2来评价。

;             (4)

;              (5)

;              (6)

.            (7)

# 2. 结果与讨论

## 2.1  嫩江组油页岩有机质热解过程解耦与单步反应动力学分析

对嫩江组油页岩有机质热解曲线按三步反应进行解耦，获得有机质热解过程与各反应在0.5、1、2、4℃/min四个升温速率下的失重速率曲线如图2所示。随着升温速率的升高，各步反应的失重过程均向右偏移，峰高与峰值温度均升高，反应发生的温度范围略有扩大，但各失重峰的相对形状与对应失重率并无明显改变。这再次说明采用该解耦方法能使对各升温速率下油页岩有机质热解过程的解耦具有一致性，保证了相同序号的拟合峰对应于同一反应，由此获得各步反应在不同升温速率下的热解失重特性，为动力学建模提供良好基础。

基于图3结果，首先采用STK方法计算各步反应在设定转化率范围内的活化能分布，结果如图2所示。三步反应的平均活化能—El分别为14.23、208.84、201.43 kJ/mol，分布范围为128.37-151.09、199.66-214.54、198.60-205.91 kJ/mol，相对标准偏差分别为3.82、1.83、2.03%。计算结果同样满足活化能均一性判据，可视作单步反应，基于该活化能，采用1.3节方法开展动力学分析，所得的各反应动力学参数最终的优化结果如表2所示。

图3 采用STK法计算的三步反应活化能分布

采用上述动力学参数对4个升温速率下各步反应过程分别进行预测，预测结果如表3所示。四个升温速率下各步反应过程的平均预测精度均超过了0.966 5，尤其是反应1和反应2（干酪根的转化过程与沥青的1次裂解）的动力学方程，平均预测精度超过0.992 9，说明建立的三个单步反应动力学方程能够较为准确地描述各个独立反应的发生过程。

表2 嫩江组油页岩有机质热解三步反应动力学参数初值与优化结果

| 参数 | 反应1 | 反应2 | 反应3 |
| --- | --- | --- | --- |
|  | 优化值 | 优化值 | 优化值 |
| E | 147.59 | 212.79 | 204.17 |
| A | 3.37E+10 | 1.38E+14 | 3.51E+12 |
| C | 1.63 | 3.76 | 3.95 |
| o | -0.36 | 0.00 | -0.44 |
| n | 1.62 | 1.20 | 1.38 |
| p | -0.08 | 0.08 | 0.75 |

表3 三步反应动力学方程对不同升温速率下各步反应过程的预测精度

| 反应 | 0.5℃/min | 1℃/min | 2℃/min | 4℃/min | 平均值 |
| --- | --- | --- | --- | --- | --- |
| 反应1 | 0.983 2 | 0.996 8 | 0.998 4 | 0.993 1 | 0.992 9 |
| 反应2 | 0.997 2 | 0.989 8 | 0.992 2 | 0.994 9 | 0.993 5 |
| 反应3 | 0.980 7 | 0.957 1 | 0.953 1 | 0.975 0 | 0.966 5 |

在获得了三步反应各自的反应动力学参数后，结合我们前期工作中探明的嫩江组油页岩热解产物分布结果[35]，可将各步反应与对应的热解产物分布进行联系。归纳三步反应产物分布时，本文将气体产物根据GC结果分为有机气体HC gases（C1-C4）和非有机气体Non-HC gases（主要为CO2、H2）两类；油产物分为四类，分别为杂原子化合物（NSO）、C10-C25的烷烃（Sat10-25）、C25以上烷烃（Sat25+）和不饱和烃（Unsat），由于绝大多数不饱和烃碳原子数小于

25，因此对不饱和烃类不再进一步细分，由此可建立三步反应的产物分布方程。在产物分布方程中，各产物的系数为产物产量占初始油页岩有机质质量的百分比，有机质质量可根据油页岩质量与TOC含量计算。在本文中，TOC含量取平均值9.01%。结合上述结果，可以分别建立三步反应的反应动力学方程与产物分布方程，从而使该动力学模型能够对嫩江组油页岩热解产物分布进行准确的预测。具体如式（8-10）所示：

反应1-干酪根的转化：

;

;

(8)

反应2-干酪根的一次裂解：

;

;

(9)

反应3-干酪根的二次裂解：

;

.

(10)

## 2.2 嫩江组油页岩的有机质热解动力学模型及评价

## 在 2.1 和 2.2 节中，我们分别得到了三步反应的反应产物分布方程和动力学方程。依据式（6）及各步反应的对应产率，各反应在有机质热解过程中的权重 wl分别为 0.229、0.509 和 0.262。将三步反应的动力学方程按照式（7）组合后，即可构建嫩江组油页岩的有机质热解动力学模型（式（11））：

.    (11)

## 结合三步反应的产物分布方程，该模型可以预测油页岩从水分蒸发阶段到有机质热解阶段的各类热解产物分布，具体如式（12）所示。其中，Ys代表 6 类油气产物的产率，即6类产物产量占初始油页岩质量的百分比，包括有机气体、无机气体和杂原子化合物等。YW,l​代表某一反应的水产率，YW,W​ 表示水分蒸发过程中的水产率。对于嫩江组油页岩，产水量为样品初始质量 m0 的 0.8%。在水分蒸发阶段（50–300℃），假设水分蒸发转化率 αW ​ 从 0 线性增加至 1，并在 300℃ 之后保持 1 不变。

;

.        (12)

为了验证所建立的有机质热解动力学模型的预测效果，计算了在 0.5、1、2、4℃/min 四种升温速率下，油页岩有机质转化率随温度变化的预测曲线，并将其与实验曲线进行对比。图 4 展示了在 0.5–4℃/min 升温速率下，动力学模型对嫩江组油页岩热解过程中有机质转化率的预测结果。可以看到，随着升温速率的增加，在有机质热解温度范围内，模型预测结果与实验数据的相关系数 R2分别为 0.997 5、0.994 8、0.998 7 和 0.998 4，平均值超过 0.997 0，表明该动力学模型在 0.5–4℃/min 的升温速率范围内具有良好的预测精度。

图4 0.5-4℃/min升温速率下嫩江组油页岩有机质热解模型预测值与实验值的对比

由上述结果可知，本文建立的油页岩多反应耦合有机质热解动力学模型由于较好地实现了多步反应的解耦，对0.5-4℃/min升温速率范围内有机质热解过程能够进行准确的预测。为验证该模型对于油页岩地下原位转化等更缓慢的升温过程同样具有良好的预测能力，采用该模型对更低升温速率（0.2℃/min）下的热解过程进行了预测，并与基于总包反应建立的热解动力学模型进行了对比。有机质热解总包反应动力学模型建模方法如下：采用0.5-4℃/min升温速率下嫩江组油页岩有机质热解阶段失重数据，参照1.3.1所列单步反应动力学分析方法建模，其中动力学参数E、A、C、o、n、p分别为282.07 kJ/mol，5.74E+18 /min，4.66，-0.390 7，-0.882 4，0.002 3，下标s代表单步总包反应。将两个有机质热解动力学模型预测的转化率变化曲线与实验曲线比较，结果如图 5 所示，图中Multi、Overall、Exp分别对应多反应耦合有机质热解动力学模型预测值、有机质热解总包反应动力学模型预测值以及实验结果。可以看到，多反应耦合有机质热解动力学模型对 0.2℃/min 升温速率下热解过程的预测精度高达 0.997，而总包反应有机质热解动力学模型预测精度仅有0.932 , 说明由于对油页岩热解过程进行了精准解耦，本文提出的有机质热解动力学模型能够更加准确描述嫩江组油页岩的有机质热解过程，并且能适用于原位转化等更加缓慢的升温历程，这一结果验证了本文所提出动力学建模方法的可靠性。

同时，基于式（12），计算了 0.2℃/min 升温速率下嫩江组油页岩在不同加热阶段的产物分布，图 5(b) 展示了油、气、水三大类产物及 6 小类油气产物产率在升温过程中的变化情况。结果表明，在 0.2℃/min 升温速率下，各类产物产率随温度升高不断增加，在 260–330℃ 之间产率缓慢增长，在 350–430℃ 之间增长最为剧烈，并最终在约 450℃ 达到峰值。具体来看，小分子烷烃与不饱和烃（HC-gases、Sat10-25 和 Unsat）的主要生成温度区间为 370–410℃，而大分子烷烃的生成区间较长，为 310–430℃。相较于其他产物，杂原子化合物和非有机气体（430℃ 之后主要为 CO₂）的生成温度更高，这意味着当加热温度超过 430℃ 时，原位转化技术的开采收益可能会下降。

| (a) | (b) |
| --- | --- |
| 图5有机质热解动力学模型对0.2℃/min升温速率下油页岩有机质热解过程转化率(a)和产物分布(b)的预测 |  |

- 结论

松辽盆地嫩江组油页岩有机质热解过程涉及多步反应的耦合，为更好地预测原位转化时有机质的缓慢热解过程及产物分布，指导该中低熟页岩油藏的高效开发，本文基于对该油页岩有机质热解过程的解耦分析进行了动力学建模，取得如下结论。

基于0.5、1、2、4℃/min升温速率下有机质热解过程的三步反应热重曲线，开展了动力学分析，确定了三步反应的活化能、指前因子与机理函数。建立的三步反应动力学方程预测精度均高于0.996。将三步反应与对应的反应产物分布进行关联，获得了嫩江组油页岩有机质热解产物分布方程。

根据各步反应在有机质热解过程中所占权重，将三步反应动力学方程进行加和，建立了油页岩多反应耦合有机质热解动力学模型。采用该模型对0.5-4℃/min升温速率范围内的油页岩热解过程进行预测，转化率预测曲线与实验结果的吻合度高于0.994。对比该模型与有机质热解总包反应动力学模型对更缓慢升温速率下（0.2℃/min）热解过程的预测精度，多反应耦合有机质热解动力学模型预测精度达到0.997，而有机质热解总包反应动力学模型的预测精度仅有0.932，说明由于对油页岩热解过程进行了精准解耦，本文提出的有机质热解动力学模型在宽升温速率范围内具有更高精度。

对嫩江组油页岩有机质热解产物分布的预测结果显示：小分子烷烃与不饱和烃的主要产生温度区间为370-410℃；大分子烷烃的主要产生温度区间较长，为310-430℃；超过430℃后嫩江组油页岩的开采效益会下降。根据不同阶段的产物组成，可以依据开采收益与加热成本来调控加热温度。

- 参考文献

[1] 金之钧, 王冠平, 刘光祥, 等. 中国陆相页岩油研究进展与关键科学问题 [J]. 石油学报, 2021, 42(7): 821-835.

JIN Z J, WANG G P, LIU G X, et al. Research progress and key scientific issues of continental shale oil in China [J]. Acta Petrolei Sinica, 2021, 42(7): 821-835. (in Chinese)

[2] Hu S, Zhao W Z, Hou L H, et al. Development potential and technical strategy of continental shale oil in China [J]. Petroleum Exploration and Development, 2020, 47(4): 877-887.

[3] 李守定, 李晓, 王思敬, 等. 页岩油化学生热原位转化开采理论与方法 [J]. 工程地质学报, 2022, 30(1): 127-143.

LI S D, LI X, WANG S J, et al. Theory and method of in-situ conversion of shale oil by chemical thermal [J]. Journal of Engineering Geology, 2022, 30(1): 127-143. (in Chinese)

[4] 金之钧, 朱如凯, 梁新平, 等. 当前陆相页岩油勘探开发值得关注的几个问题 [J]. 石油勘探与开发, 2021, 48(6): 276-1287.

JIN Z J, ZHU R K, LIANG X P, et al. Several issues worthy of attention in current lacustrine shale oil exploration and development [J]. Petroleum Exploration and Development, 2021, 48(6): 1276-1287. (in Chinese)

[5] Zou C N, Pan S Q, Jing Z H et al. Shale oil and gas revolution and its impact[J].Acta Petrolei Sinica, 2020, 41(1):1-12.

[6] Zhao W Z, Hu S Y, Hou L H, et al. Types and resource potential of continental shale oil in China and its boundary with tight oil [J]. Petroleum Exploration and Development, 2020, 47(1): 1-11.

[7] Zhao W Z, Hu S Y, Hou L H. Connotation and strategic role of in-situ conversion processing of shale oil underground in the onshore China [J]. Petroleum Exploration and Development, 2018, 45(4): 563-572.

[8] 崔景伟, 侯连华, 朱如凯, 等. 鄂尔多斯盆地延长组长7页岩层段岩石热导率特征及启示 [J]. 石油实验地质, 2019, 41(2): 280-288.

CUI J W, HOU L H, ZHU R K, et al. Thermal conductivity characteristics of rocks in the Chang 7 shale layer of the Yanchang Formation in the Ordos Basin and their implications [J]. Petroleum Experimental Geology, 2019, 41(2): 280-288. (in Chinese)

[9] Aboulkas A, El Harfi K. Study of the kinetics and mechanisms of thermal decomposition of Moroccan Tarfaya oil shale and its kerogen [J]. Oil Shale, 2008, 25(4): 426-443.

[10] Sütcü H. Pyrolysis kinetics of oil shale from Urukisla, Turkey [J]. Oil Shale, 2009, 26(4): 491-499.

[11] 梁鲲, 梁杰, 史龙玺, 等. 升温速率对桦甸油页岩热解特性及动力学的影响 [J]. 矿业科学学报, 2018, 3(2): 194-200.

LIANG K, LIANG J, SHI L X, et al. Effects of heating rate on the pyrolysis characteristics and kinetics of Huadian oil shale [J]. Journal of Mining Science and Technology, 2018, 3(2): 194-200. (in Chinese)

[12] Li S, Yue C. Study of pyrolysis kinetics of oil shale [J]. Fuel, 2003, 82(3): 337-342.

[13] Bai F, Guo W, Lü X, Liu Y, Guo M, Li Q, et al. Kinetic study on the pyrolysis behavior of Huadian oil shale via non-isothermal thermogravimetric data [J]. Fuel, 2015, 146: 111-118.

[14] Bai F, Sun Y, Liu Y, Guo M, Zhao J. Characteristics and kinetics of Huadian oil shale pyrolysis via non-isothermal thermogravimetric and gray relational analysis [J]. Combustion Science and Technology, 2020, 192(3): 471-485.

[15] Moine EC, Bouamoud R, El Hamidi A, Khachani M, Halim M, Arsalane S. Mineralogical characterization and non-isothermal pyrolysis kinetics of Moroccan Rif oil shale [J]. Journal of Thermal Analysis and Calorimetry, 2018, 131(2): 993-1004.

[16] Pan N, Li D, Lü W, Dai F. Kinetic study on the pyrolysis behavior of Jimsar oil shale [J]. Oil Shale, 2019, 36(4): 462-482.

[17] Liu Q, Han X, Li Q, Huang Y, Jiang X. TG–DSC analysis of pyrolysis process of two Chinese oil shales [J]. Journal of Thermal Analysis and Calorimetry, 2014, 116: 511-517.

[18] Abu El-Rub Z, Kujawa J, Al-Gharabli S. Pyrolysis kinetic parameters of Omari oil shale using thermogravimetric analysis [J]. Energies, 2020, 13(16): 40-60.

[19] Zhao S, Su J, Wu J. Release performance and kinetic behavior of volatile products from controlled pressure pyrolysis of oil shale in nitrogen atmosphere [J]. Scientific Reports, 2023, 13: 10676.

[20] 张丽丽, 徐龙, 马晓迅. 应用TG-FTIR法研究铜川油页岩的热解特性 [J]. 化工进展, 2011, 30(S1): 115-119.

ZHANG L L, XU L, MA X X. Tongchuan oil shale pyrolysis by TG-FTIR [J]. Chemical Industry and Engineering Progress, 2011, 30(S1): 115-119. (in Chinese)

[21] 王擎, 闫宇赫, 贾春霞, 等. 甘肃油页岩红外光谱分析及热解特性 [J]. 化工进展, 2014, 33(7): 1730-1734+1768.

WANG Q, YAN Y H, JIA C X, et al. FTIR analysis and pyrolysis characteristics of oil shale from Gansu province [J]. Chemical Industry and Engineering Progress, 2014, 33(7): 1730-1734+1768. (in Chinese)

[22] Ryan RC, Fowler TD, Beer GL, Nair V, Ogunsola OI, Hartstein AM, Ogunsola O. Shell’s in situ conversion process—from laboratory to field pilots [M]. In: Oil Shale: A Solution to the Liquid Fuel Dilemma; American Chemical Society: Washington DC, 2010.

[23] Jiang H Y, Liu S, Wang J, You Y, Yuan S B. Study on evolution mechanism of the pyrolysis of Chang 7 oil shale from Ordos Basin in China [J]. Energy, 2023, 272: 127097.

[24] You Y L, Han X X, Wang X Y, Jiang X M. Evolution of gas and shale oil during oil shale kerogen pyrolysis based on structural characteristics [J]. Journal of Analytical and Applied Pyrolysis, 2019, 138: 203-210.

[25] You Y, Han X, Liu J G, Jiang X M. Structural characteristics and pyrolysis behaviors of Huadian oil shale kerogens using solid-state 13C NMR, Py-GCMS, and TG [J]. Journal of Thermal Analysis and Calorimetry, 2018, 131(2): 1845-1855.

[26] Wang Q, Wang X M, Pan S. Study on the structure, pyrolysis kinetics, gas release, reaction mechanism, and pathways of Fushun oil shale and kerogen in China [J]. Fuel Processing Technology, 2022, 225: 107058.

[27] Chen B, Han X X, Li Q Y, Jiang X M. Study of the thermal conversions of organic carbon of Huadian oil shale during pyrolysis [J]. Energy Conversion and Management, 2016, 127: 284-292.

[28] 陆梦科, 匡吴奇, 钱刚, 等. 美国绿河油页岩中沥青热解特征及动力学 [J]. 化工学报, 2018, 69(11): 4746-4753.

LU M K, KUANG W Q, QIAN G, et al. Pyrolysis characteristics and kinetics of bitumen from Green River oil shale [J]. Journal of Chemical Industry and Engineering, 2018, 69(11): 4746-4753. (in Chinese)

[29] 王擎, 关京, 徐芳. 油页岩热解特性及其甲烷释放规律研究 [J]. 化工学报, 2018, 69(10): 4362-4370.

WANG Q, GUAN J, XU F. Pyrolysis characteristics of oil shale and analysis of methane evolution mechanism [J]. Journal of Chemical Industry and Engineering, 2018, 69(10): 4362-4370. (in Chinese)

[30] Baruah B, Kataki R, Thakur P, Tiwari P. Detailed physicochemical and thermochemical investigation of Upper Assam oil shale [J]. Journal of Thermal Analysis and Calorimetry, 2019, 138(2): 1221-1232.

[31] Zhang J, Ding Y M, Du W Z, Lu K H, Sun L L. Study on pyrolysis kinetics and reaction mechanism of Beizao oil shale [J]. Fuel, 2021, 296: 120696.

[32] Bai F T, Sun Y H, Liu Y M, Li Q, Guo M Y. Thermal and kinetic characteristics of pyrolysis and combustion of three oil shales [J]. Energy Conversion and Management, 2015, 97: 374-381.

[33] Ding H S, Ma Y, Li S Y, Wang Q, Hong W P, Jiang H F, et al. Pyrolytic characteristics of Fushun oil shale and its by-products [J]. Journal of Thermal Analysis and Calorimetry, 2022, 147(8): 5255-5267.

[34] Alves JLF, da Silva JCG, Mumbach GD, Di Domenico M, Marangoni C. Assessing the potential of the invasive grass Cenchrus echinatus for bioenergy production: A study of its physicochemical properties, pyrolysis kinetics and thermodynamics [J]. Thermochimica Acta, 2023, 724: 179500.

[35] Xiong C, Chen J Y, Xu R N, Song Q. Pyrolysis characteristics and mechanism of oil shale in the Songliao Basin of China [J]. Fuel, 2025, 386: 134251.

[36] Starink MJ. The determination of activation energy from linear heating rate experiments: a comparison of the accuracy of isoconversion methods [J]. Thermochimica Acta, 2003, 404(1): 163-176.

[37] Coats AW, Redfern JP. Kinetic parameters from thermogravimetric data [J]. Nature, 1964, 201(4914): 68-69.

[38] Zhang Z Q, Duan H Q, Zhang Y J, Guo X J, Yu X, Zhang X G, et al. Investigation of kinetic compensation effect in lignocellulosic biomass torrefaction: Kinetic and thermodynamic analyses [J]. Energy, 2020, 207: 118290.

[39] Mumbach GD, Alves JLF, da Silva JCG, Domenico MD, Arias S, Pacheco JGA, et al. Prospecting pecan nutshell pyrolysis as a source of bioenergy and bio-based chemicals using multicomponent kinetic modeling, thermodynamic parameters estimation, and Py-GC/MS analysis [J]. Renewable and Sustainable Energy Reviews, 2022, 153: 111753.

[40] Friedman HL. Kinetics of thermal degradation of char-forming plastics from thermogravimetry. Application to a phenolic plastic [J]. Journal of Polymer Science Part C: Polymer Symposia, 1964, 6(1): 183-195.

[41] Vyazovkin S, Burnham AK, Criado JM, Pérez-Maqueda LA, Popescu C, Sbirrazzuoli N. ICTAC Kinetics Committee recommendations for performing kinetic computations on thermal analysis data [J]. Thermochimica Acta, 2011, 520(1): 1-19

[42] Vyazovkin S, Burnham AK, Favergeon L, Koga N, Moukhina E, Pérez-Maqueda LA, et al. ICTAC Kinetics Committee recommendations for analysis of multi-step kinetics [J]. Thermochimica Acta, 2020, 689: 178597.

[43] Bai F T, Liu Y, Lai C, et al. Thermal degradations and processes of four kerogens via thermogravimetric–Fourier-transform infrared: Pyrolysis performances, products, and kinetics [J]. Energy & Fuels, 2020, 34(3): 2969-2979.

Kinetic model for the pyrolysis of organic matter in oil shale from the Nenjiang Formation, Songliao Basin

Abstract：The medium-low maturity shale oil reservoirs in the Nenjiang Formation of the Songliao Basin in China have significant development potential. In-situ conversion technology is considered the most promising method for extracting oil from such reservoirs. The conversion process involves multiple coupled pyrolysis reactions of the oil shale. Therefore, a pyrolysis kinetic model capable of predicting these reactions and the distribution of pyrolysis products is crucial for the effective application of in-situ conversion technology in this oil reservoir. In this study, the organic matter pyrolysis process of oil shale from the Nenjiang Formation was decoupled into three distinct reactions based on deconvolution analysis of the derivative thermogravimetry (DTG) curves obtained from pyrolysis experiments conducted at heating rates of 0.5, 1, 2, and 4 °C/min. Kinetic analysis was conducted for the three reactions, and the resulting kinetic equations demonstrated prediction accuracies greater than 0.96 for each reaction process. A kinetic model for the pyrolysis of organic matter in oil shale from Nenjiang Formation was established by incorporating the product distribution of each reaction and their respective weights in the pyrolysis process. This model demonstrated high prediction accuracy (R² > 0.994) for the pyrolysis process of organic matter at heating rates ranging from 0.2 to 4 °C/min, significantly outperforming the global reaction kinetic model (prediction accuracy of 0.932). As a result, this kinetic model can be used to predict the pyrolysis process and product distribution of organic matter under various heating conditions, providing valuable guidance for the development of in-situ conversion technology for this shale reservoir.

Keywords：medium-low maturity shale oil；in-situ conversion；pyrolysis；deconvolution；kinetic model；chemical reaction.